|  | # Enclosure CV-CAMP OS 26x80 IP54 RAL 3000 |
| --- | --- |
| General information |  |
| Model | SONDER-FP745 |
| EAN |  |
| Product batch designation | CAMP |
| Manufacturer | DOKTORVOLT |
| Enclosure specifications |  |
| Enclosure dimensions | 80 x 26 x 24 cm |
| Enclosure material | SMC slow-burning and self-extinguishing composite: (polyester + glass fibre) |
| Enclosure colour | RED RAL3000 |
| Protection grade IP rating | IP54 |
| Impact resistance | IK10 |
| Flammability category | V0 |
| Rated insulation voltage | 690 V |
| Temperature operating conditions | -50 ~ +85°C |
| Protection class | II |
| Dielectric strength | 22kV/mm |
| Resistivity | 1014Ωcm |
| Tracking resistance | CTI 600 |
| UV resistance | yes |
| Stationary design | yes |
| Conformity |  |
| Enclosure: Manufacturer certifications and standards | PN-EN 61439-1:2011, PN-EN 61439-5:2015-02 PN-EN 60529:2003, PN-EN 62208:2003 |