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	Enclosure CV-CAMP OS 26x80 IP54 RAL 3000


	General information	
	       

	Model
	SONDER-FP745

	EAN
	

	Product batch designation
	CAMP

	Manufacturer
	DOKTORVOLT

	
	

	Enclosure specifications
	

	Enclosure dimensions
	80 x 26 x 24 cm

	Enclosure material
	SMC slow-burning and self-extinguishing composite: (polyester + glass fibre)

	Enclosure colour
	RED RAL3000

	Protection grade IP rating
	IP54

	Impact resistance
	IK10

	Flammability category
	V0

	Rated insulation voltage
	690 V

	Temperature operating conditions
	-50 ~ +85C

	Protection class
	II

	Dielectric strength
	22kV/mm

	Resistivity
	1014Ωcm

	Tracking resistance
	CTI 600

	UV resistance
	yes

	Stationary design
	yes

	
	

	Conformity
	

	Enclosure: Manufacturer certifications and standards
	PN-EN 61439-1:2011, PN-EN 61439-5:2015-02
PN-EN 60529:2003, PN-EN 62208:2003
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